## Slide 1: ROSE meeting 24th-27th April 2017
PhD student: Serhii Lozovyi
Supervisor: Prof. Andreas Bauer
Acknowledgments: Tore Sirevaag, Erling Fjær
The relation between static and dynamic stiffness of rocks
24.04.2017
Trondheim, Norway
Notes: OK

## Slide 2
Elastic media:
Stiffness does not depend on frequency or stress amplitude
Static stiffness = dynamic stiffness
Rocks are not elastic media
Stiffness of rocks depends on frequency and strain amplitude
Static stiffness  dynamic stiffness
Static stiffness depends on stress amplitude (often ignored in geomechanical modeling)
Acoustic velocities (dynamic stiffness) depend on amplitude (non-linear acoustics)
We propose and validate a simple model that relates static and dynamic rock stiffness and describes the dependence of the rock stiffness on stress amplitude

## Slide 3: Basics
Dynamic stiffness (seismic, sonic, ultrasonic): µstrain amplitudes
(Quasi-)Static stiffness: mstrain amplitudes
H
G
Edyn
νdyn
P-wave modulus
Young's modulus
Poisson's ratio
Shear modulus
σ
εax εrad
Estatic
νstatic
Strains
Stress
Young's modulus
Poisson's ratio
Velocities

## Slide 4: Why does the static undrained stiffness differ from the dynamic stiffness?
Stress amplitude
 Activation of non-elastic processes (focus of this work);
Strain rate / frequency
 dispersion effects
average strain rate of a wave:
f – frequency
ε0 – strain amplitude

## Slide 5: Non-elastic process
– friction is suppressing intergranular movement
– sliding is activated
– friction is reactivated after the change in loading direction

## Slide 6: Real experiment Undrained unloading/loading cycles

## Slide 7: Model by Fjær et al. (2013)
Non-elastic compliance
dispersion
constants
Non-elastic compliance tends to increase linearly from the start of the unloading;
Empirical model was confirmed in experiments with sandstones and shales;
No data available in the vicinity of turning point (small z) due to experimental constrains.
slope
E – local Young's modulus during unloading
Edyn – dynamic (elastic) Young's modulus
– axial stress change
unloading
A
B
z

## Slide 8: Low frequency apparatus
Ultrasonic P- and
S-wave transducers
Rubber sleeve
Strain gauges
Pore pressure channels
Sample
Force sensor
Piezoelectric
actuator
Internal load
sensor for static
Static force from a
loading frame
Confining
pressure
Measurements on the same core:
Static moduli
Low frequency Young’s modulus and Poisson’s ratio (0.1-150 Hz)
Ultrasonic velocity (500 kHz)
Very sensitive to small (order of 10-6) strains,
stress amplitude is a variable in a relatively wide range
Axial stress (σax) modulations are applied
Axial () and radial () strains are recorded

## Slide 9: Static unloading and low frequency oscillations at various stress amplitudes (0÷0.5 MPa)
Stress path
Compliance
Water-saturated Castlegate sandstone
Strain rate during unloading is similar to average strain rate of dynamic measurement  dispersion can be neglected

## Slide 10: Dispersion effects
Water-saturated Castlegate sandstone
For Castlegate sandstone, the difference between static and dynamic stiffness is due to the larger stress amplitude at static measurements
Dispersion effects are relatively small

## Slide 11: Shales are highly inelastic and dispersive: Example Opalinus clay
Stress amplitude: 2 MPa
Stress amplitude: 1 MPa
Stress amplitude: 4 MPa
E [Gpa] |  | 
(1MPa) | (2MPa) | (4MPa)
4.3 | 3.3 | 2.3
4.8 | 5.0 | 4.8
Average Stress-strain slope
Zero-strain extrapolation

## Slide 12: Young's modulus dependance on stress amplitude and frequency
1 Mpa
Stress amplitude
2 Mpa
4 Mpa
Opalinus clay
-53%

## Slide 13: Conclusions
Rocks are non-elastic for strains > 1 strain, both during loading and unloading
With decreasing stress/strain amplitude, the static undrained stiffness approaches the dynamic stiffness if dispersion effects can be neglected
For some rocks (e.g. Opalinus Clay), non-elastic effects are large, and the typical assumption of quasi-elastic behavior (constant stiffness) up to a yield/failure point may result in significant errors in geomechanical models.
A simple model was proposed that relates dynamic and static stiffness of rocks and describes the dependence of the rock stiffness on stress amplitude, and that could easily be implemented in geomechanical models.